## Slide 1
Material selection on H2 ready well infrastructures
IGU –UGS Committee meeting
Chongqing 11th-13th Octobre 2023

## Slide 2
Test results on cements
Repurposing of current asset to H2-GN blends

## Slide 3: Test results on cements
Cement is classified as a»primary barrier» according Well intgrity management practice because:
It is directly in contact with hydrocarbons
restore the integrity of the caprock behind the casing
But also prevent flows through annular space between casing and wellbore
Studies on cement behaviour are as fundamental as studies on steell HE
Tubing
di iniezione
erogazione
gas
Testa Pozzo
Valvola di sicurezza
Packer
Filtri
Gravel Pack
Giacimento
Tubo Guida
Casing intermedio e di produzione
Casing Superficiale
Roccia di copertura
DHE
Cemento
Cement

## Slide 4: Cements H2 test results (SPE-214423-MS Snam- Stratum –Loeben univ.)
H2 behaves like an inherts into the cement and any significant change was detectet in its properties
“ An Interdisciplinary Approach to Investigate the Cement Integrity for Underground Hydrogen Storage Wells”
3 Types of cements tested :
API class A
API class G
Special cement blend

## Slide 5: Cements results 2

## Slide 6: Cements results 3

## Slide 7: Cements results 4

## Slide 8: Repurposing current UGS well stock to H2-GN blend
Tricky topic: for hundreds of well, it needs to know
  Well history
  Detailed list of materials utilised
  What has been going in and out for decades
  Tubing casing corrosion(?)
  Is there any third party company that can certify a well can be repurposed?
Mean age of our well stock is more than 30 years: repurposing is a very important topic in terms of strategy, investment planning
Tubing
di iniezione
erogazione
gas
Testa Pozzo
Valvola di sicurezza
Packer
Filtri
Gravel Pack
Giacimento
Tubo Guida
Casing intermedio e di produzione
Casing Superficiale
Roccia di copertura
DHE
Cemento

## Slide 9: Snam strategy for asset repurposing up to 10%H2-NG blend
WIMS
Certification of well integrity management system (WIMS) according to ISO 16530 from an external certification body
Material testing
Complete testing on materials rtrieved from old wells (valves , casing, elastomers)
Field assessment
Site specific well assessement in order to verify all information about materials are available

## Slide 10: Repurposing current UGS well stock to H2-GN blend: test on new materials can be used for old wells?
From Hystories released information
Resource: Hystories_D4.6-0-Summary-report-on-all-investigated-steels.pdf
Focus on J55 (most diffused materials on production tubing in Italy) and P110 (present on ancillary completion equipment).
Mechanic test =CLT constant load test
Hydrogen pressure = 100 and 120 bar
Environment: with and without
1%H2S, 13% CO2, brine
Room temperature
Positive results for almost all tested materials

## Slide 11: Repurposing current UGS well stock to H2-GN blend: test on new materials can be used for old wells?
P110 : usable at room temperature without H2S, but the test at RT (with H2S) was positive.
J55 : applicable, but ISO 15156-2 clause 8 highlights HIC problems at RT (minor issues on new pipes but on 30 years old pipe ?)
Main impurity that enhancing HE are sulphur inclusions and shape of steel microstructure.
Unfortunately P110 J55 idientify material classes and chemically composition is not very well detailed.
Control of impurity like sulphur in steel farm has drastically improved through years: P110 produced in ’70s probably would fail the test proposed in Hystories
Well Repurpsing requires a deep knowledge of our well stock, and very good data traceability.
HIC
HSC or SSC